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Product overview
Vibratory polishing is used to reduce the fine deformation layer left by mechanical preparation and improve the specimen surface finish. The ZDP-300 is intended for preparation ahead of EBSD, AFM and SEM analysis. Its mechanical-chemical polishing action is particularly suited to soft and ductile materials, including titanium, aluminium and copper and their alloys, as well as nickel-based alloys and high-temperature alloys.
Specifications
	Model
	ZDP-300

	Machine body configuration
	Benchtop

	Control method
	Touchscreen control

	Polishing disc size
	305 mm

	Polishing diameter
	Φ8-50 mm (custom sizes available)

	Main unit power
	1.5 KW

	Frequency adjustment
	automatic  (0-400Hz adjustable )

	Voltage adjustment
	automatic  (0-220V adjustable )

	Power supply
	220V

	Dimensions
	500*480*320 mm (L * W * H)

	Net weight
	59.5 KG

	Gross weight
	70 KG

	Standard configuration
	

	Main unit
	1 unit

	Transparent dust cover
	On main unit

	Specimen holder
	3 sets each of Φ25/30/40 mm; holds mounted or unmounted specimens

	Polishing consumables
	1 final polishing cloth, 1 bottle of 0.05 μm alumina powder, 1 bottle of 0.02 μm silica suspension

	Counterweights
	2 pieces

	Level vial
	1 piece

	Power cable
	1 piece

	Technical documentation
	1 set (manual, inspection certificate and warranty card)


Contact
Phone: 400-8127-833 / +86-21-58391850
Email: shanghai@yr17.net
Address: No.1478 Nanfeng Highway, Fengxian District, Shanghai, China
Website: www.cnnoet.com
Compiled from published product information. Final configuration follows the technical agreement; confirm options, fixtures and scope with an application engineer.
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